Standard Operating Procedure: Thin Section Sample Preparation

Author: Will Haddick

Objective:

To convert raw stone material into thin sections 30 µm thick to be used for petrographic and EMPA analysis.

Procedure:

- Using a 150 grit (93 µm) Buehler Ecomett III diamond grinding wheel, grind samples by hand to achieve a uniform flat surface.

- Grind samples by hand again using a 280 grit (43µm) Buehler Ecomett IV diamond grinding wheel to secure a flat sample surface.

- Using a Diamond Pacific grinding belt at 150 grit (93 µm), round off sharp sample corners and create a 45° bevel on all four sample edges.

- Rinse samples with water and set to dry in a drying oven at 100° C for approximately 5 minutes.

- Place glass slides frosted side facing down on top of a hot plate set to 200° C.

- Create an epoxy/resin mix by adding 3.5 g Hillquist resin with 1.5 g Hillquist hardener and mixing throughouly, set in drying oven for approximately 2 minutes.

- Take one dry sample out of the drying oven, and spread the even epoxy/resin mix evenly over the flat surface that was ground flat by hand.

- Take one glass slide off of the hot plate, and gently lower frosted side down onto the sample coated with epoxy/resin.

- Using a circular motion, move any bubbles trapped within the epoxy/resin outwards towards the sample edge and away from the glass slide.

- Place sample glass side facing down onto a level surface, allow to dry at a minimum of 24 hours, and repeat steps 6-8 with remaining samples.

- Once dry, engrave the sample ID number onto the glass slide using a diamond tipped engraving pen.

- Using a Buehler Petro Thin thin sectioning system, grind samples down to ~250 µm in thickness at 250 µm increments. If samples are too thick to be placed into the Petro Thin, cut the stone side of the sample using a circular saw to the desired length to fit.

- Grind samples by hand on a RatioPax DC Motor Control grinding wheel using 220 grit (68 µm) silicon carbide powder to achieve a thickness of 140 µm.

- Grind sample down again on the RatioPax wheel using 400 grit (22 µm) silicon carbide powder to qualitatively ensure feldspars appear a burnt-orange color on a Michelle Levy Bifrengence color chart, when looked at underneath cross polarized light on a petrographic microscope. Samples should not fall below 135 µm in thickness.

- Take samples back to the Diamond Pacific grinding belt and round off GLASS corners of each sample using a 15 grit  belt.